## Slide 2: Failure Prediction Mechanism for Pluggable Optical Interconnect at Facebook Data Centers
Abhijit Chakravarty and Vincent Zeng

## Slide 3: Problem Statements
Currently there is no method developed to avoid the optical transceiver failures ahead of time. Network traffic loss is not predicable

## Slide 4: Real-time performance monitoring mechanism at FB data centers
Temperature Readout
By data centers
By suppliers
By part number
By switch port
Over time
All switch platforms (RSW = rack switch, FSW = fabric switch, ESW = edge switch, SSW = spine switch)
Temperature, Tx Bias, Tx Power, Vcc, Rx Power
Transmitter Power Readout
Tx Bias Current Readout

## Slide 5: Real-time monitoring mechanism implementation at our DCs
Shows the relationship between tx/rx power, current, and temperature
As a transceiver degrades/begins to fail, current gradually increases to maintain steady Tx Power, until reaching a plateau at 65mA (depends on supplier)
Beyond the plateau, recovery is impossible and the particular transmitter will likely fail in a few
Also, the case temperature has a positive correlation with transmitter bias current and negative correlation with transmitter optical power
This correlation can help us better predict the failures and prevent the link failure in a data center before it actually occurs

## Slide 6: Failure Modes Observation
~20 units were pulled
All of them failed after stressful test within two weeks

## Slide 7: Some Basic Of Laser Diode Failures
Power Reduction
Wavelength shift
Spectral linewidth widening
Modulation speed change
No lasing suddenly
Defect/dislocation propagates
Metal diffusion/mitigation. Defect propagates
Grating area disorder/precipitation/facet melting
Defect propagates/grows
Bonding part/alloy reaction/thermal fatigue

## Slide 8: Algorithm Proposed
The adjustment of the sensitivity of top power monitoring (TPM device)
Need to set the algorithm to find out the saturation of Tx power output.

## Slide 9: Conclusions
We investigated the correlation among the bias current of the laser diode, transmitter power degradation and environmental changes.
We identified signatures for laser diode degradation
We are developing a mechanism to predicate the failure modes.